## Slide 1: Simulation of grain morphology evolution during sintering
Evan Pereira (2nd year Ph.D)
Jacques Léchelle, Adrien Socié, Luca Messina – CEA Cadarache IRESNE
François Valdivieso, Julien Bruchon – Ecole des Mines Saint-Etienne
Gaelle Raveu, Maelys Gauthé – Framatome

## Slide 2: Introduction
1

## Slide 3: Context : Nuclear Fuel
In France 65% of the electricity come from the nuclear industry.
3rd rank in term of production in the world (380.5 TW/h or 13.5%) after the USA and China
2nd in installed power (63 GW or 16.8%) after the USA
57 Pressurized Water Reactors across the country [1,2]
The fuel is constituted of cylinders pellets of sintered and (about ~13mm in height, ~8mm width and ~7.5g)
Pellets are put in 4m long fuel rods organized in assemblies
[1] 2025 Statistical Review of World Energy, Energy Institute
[2] 2025 World Statistic International Atomic Energy Agency
[3] Framatome Romans R&D presentation
[4] World nuclear association https://world-nuclear.org/information-library
[4]
[4]
[3]
Notes: ENVIRON

## Slide 4: Accident Tolerant Fuels
Current developments in nuclear fuels are aimed at Accident Tolerant Fuel technologies, to enhance safety and performance.
One of them is Chromia-doped fuel pellets, to retain fission gases better and improve pellet-cladding interaction.
UO2+0.1 wt% Cr2O3
UO2+0.25 wt% Cr2O3
Cr2O3 doped UO2
Pure UO2
Bigger grains, which improves fission gas retention [1]
More radial cracks in the periphery of doped UO2 → relieve of stress [2]
[2] Nonon et al., PCI Behaviour of Chromium Oxide-Doped Fuel, OECD, Nuclear. Energy Agency, 2005
[1] L. Bourgeois and al., Factors governing microstructure development of Cr2O3-doped UO2 during sintering, Journal of Nuclear Materials, 2001
Potentiellement slide bonus
Notes: Ph. D. topic : sintering model accounting for different interspecies diffusion (U, Cr) and initial morphology

## Slide 5: Context : Manufacturing of fuel pellets
Pellet manufacturing is one of the last steps of the fuel production.
The entire heating cycle takes around 24 hours, in a furnace at around 1700°C with reducing atmosphere
raw material
Powder preparation
powder
Pressing
Compact mass
Sintering
pellet
Regrinding
Coating and assembly
~500 MPa
Reducing Gas Atmosphere ()
Vaporisation of organics ()
Reduction
Sintering
Cooling
E. Pereira - Simulation of grain morphology evolution during sintering
Framatome Romans R&D presentation
Notes: Référence framatome

## Slide 6: CEA simulation and multiscale approach to sintering
VER
VER
Microscopic
Mesoscopic
Macroscopic
Numerical
Pellet
Defect formation during sintering
Impact of heterogeneities
Oxygen transport
RVE
Modelling grain growth
Material diffusion
Thesis N. Dempowo (2022)
Crystallites/grains
Salammbo
Homogenization
Microstructural changes
Thesis S. Martin (2014)
Furnace…
Thesis A. Ouhammou (2025)
6
Model feeding
E. Pereira - Simulation of grain morphology evolution during sintering
High density
Low density
High density
Notes: a traduire

## Slide 7: CEA simulation and multiscale approach to sintering
VER
VER
Microscopic
Mesoscopic
Macroscopic
Numerical
Pellet
Defect formation during sintering
Impact of heterogeneities
Oxygen transport
RVE
Thesis N. Dempowo (2022)
Crystallites/grains
Salammbo
Homogenization
Microstructural changes
Thesis S. Martin (2014)
Ph.D. topic : simulation from 2 crystallites to RVE
Furnace…
Thesis A. Ouhammou (2025)
2 grains
Multi-grain
RVE
7
Model feeding
Modelling grain growth
Material diffusion
E. Pereira - Simulation of grain morphology evolution during sintering
High density
Low density
High density
Notes: a traduire

## Slide 8: CEA simulation and multiscale approach to sintering
VER
VER
Microscopic
Mesoscopic
Macroscopic
Numerical
Pellet
Defect formation during sintering
Impact of heterogeneities
Oxygen transport
RVE
Ph.D. N. Dempowo (2022)
Crystallites/grains
Salammbo
Homogenization
Microstructural changes
Ph.D. S. Martin (2014)
Furnace…
Ph.D. A. Ouhammou (2025)
8
Model feeding
Presentation topic : working on two interface evolution methods: phase field and adaptive meshes
Ph.D. topic : simulation from 2 crystallites to RVE
Modelling grain growth
Material diffusion
E. Pereira - Simulation of grain morphology evolution during sintering
High density
Low density
High density
Notes: a traduire

## Slide 9: Models
2

## Slide 10: Hypothesis
Initial time :
  Temperature : 800–900 degrees
  Chromium : already solubilized in some grains
  Reduction to UO₂ at low temperature completed
  Generation of an initial microstructure using a set of spheres
Overall evolution in the RVE :
  O/M and temperature evolve uniformly across the domain
  Effect of the dopant, modification of some/every diffusion coefficients
Considerations about the study domain (RVE) :
  Aimed to solve several thousand of Degrees of Freedom
  Evolving boundary conditions due to shrinkage
L
L’
Merope: A microstructure generator for simulation of heterogeneous materials, M. Josien, 2024
E. Pereira - Simulation of grain morphology evolution during sintering
Notes: Citer merope

## Slide 11: Multi-physics problem
Mechanical problem :
Static equilibrium :
Infinitesimal strain :
Laplace-Young’s law :
E. Pereira - Simulation of grain morphology evolution during sintering
11
Compression
Tension
Compression

## Slide 12: Multi-physics problem
Chemical problem :
Fick’s law :
Multi-species transport :
Mechanical problem :
Static equilibrium :
Infinitesimal strain :
Laplace-Young’s law :
E. Pereira - Simulation of grain morphology evolution during sintering
12
Compression
Tension
Compression

## Slide 13: Multi-physics problem
Mechanical problem :
Static equilibrium :
Infinitesimal strain :
Laplace-Young’s law :
Multiphysics coupling:
E. Pereira - Simulation of grain morphology evolution during sintering
Chemical problem :
Fick’s law :
Multi-species transport :
13
Compression
Tension
Compression
Notes: RAJOUTER IMAGE ANGLE DIEDRE

## Slide 14: Interface evolution
FE Adaptive meshes [1]
Based directly on constitutive laws
Lagrangian, dynamic evolution of the mesh of the surface of the grains
Continuity of the flux :
E. Pereira - Simulation of grain morphology evolution during sintering
14
[1] J. Léchelle and al. «A sub-granular scale model for solid state free sintering: results on the evolution of two grains», Journal of chemical technology and metallurgy, 2014
Notes: Lier avec slide 13
Intégrale en grand

## Slide 15: Interface evolution
FE Adaptive meshes [1]
Based directly on constitutive laws
Lagrangian, dynamic evolution of the mesh of the surface of the grains
Continuity of the flux :
Phase-field modelling [2]
Eulerian, evolution of the fields on a fixed mesh
The interfacial energy between grains does not depend on the thickness of the continuous interfaces
Total Grand Potential energy :
Allen-Cahn (grains and porosity phase) : &
Cahn-Hilliard (diffusion) :
E. Pereira - Simulation of grain morphology evolution during sintering
[2] I. Greenquist and al. «Development of a microstructural grand potential-based sintering model», Computational Materials Science, 2020
[1] J. Léchelle and al. «A sub-granular scale model for solid state free sintering: results on the evolution of two grains», Journal of chemical technology and metallurgy, 2014
15
Notes: Lier avec slide 13
Intégrale en grand

## Slide 16: CEA Software algorithm
SALAMMBO : FE Adaptive meshes [1]
Stress field calculation
Material flows calculation
Material balance on surface triangles
Displacement of surface nodes
Smoothing of the surface mesh
Remeshing of the volume
Interfaces evolution
Lagrangian approch
Thermodynamic section
2D Finite Volume solving
Mechanical section
3D Finite Element solving
E. Pereira - Simulation of grain morphology evolution during sintering
16
[1] J. Léchelle and al. «A sub-granular scale model for solid state free sintering: results on the evolution of two grains», Journal of chemical technology and metallurgy, 2014
Notes: Traduire salammbo

## Slide 17: CEA Software algorithm
SALAMMBO : FE Adaptive meshes [1]
INFERNO : Phase-field modelling [3]
Calculation of the order parameters at
Calculation of the order parameters at 𝑡_(𝑖+1)
Calculation of the chemical potential at
Calculation of the chemical potential at 𝑡_(𝑖+1)
Constraints on the chemical potential
Computation of the new system state
Calculations of fields derivatives at
Calculations of fields derivatives at 𝑡_𝑖
Constraints on the chemical potential
Computation of the new system state
Stress field calculation
Material flows calculation
Material balance on surface triangles
Displacement of surface nodes
Smoothing of the surface mesh
Remeshing of the volume
Interfaces evolution
Lagrangian approch
Thermodynamic section
2D Finite Volume solving
Mechanical section
3D Finite Element solving
E. Pereira - Simulation of grain morphology evolution during sintering
17
[3] L. Messina, “Phase-field modeling and benchmark of microstructure evolution in polycrystalline UO2 with the INFERNO code”, presented at the NuFuel conference, Delft, the Netherlands, Sept 18, 2025.
Stress field calculation
Material flows calculation
Material balance on surface triangles
Displacement of surface nodes
Smoothing of the surface mesh
Remeshing of the volume
Interfaces evolution
Lagrangian approch
Thermodynamic section
2D Finite Volume solving
Mechanical section
3D Finite Element solving
[1] J. Léchelle and al. «A sub-granular scale model for solid state free sintering: results on the evolution of two grains», Journal of chemical technology and metallurgy, 2014
Notes: NOM DES METHODES : adaptive meshes et phase field

## Slide 18: Results : Salammbo
  [1]
E. Pereira - Simulation of grain morphology evolution during sintering
Validation on CeO2
  [1]
  [2]
18
[1] Ph.D. S. Martin, 2014, « Contribution to the modelling of solid state sintering »
[2] Ph.D. G. I. Nkou Bouala, 2016, «First step of sintering of lanthanides and actinides oxides : an in situ study by ESEM at high temperature»
Notes: Matériau homogène

## Slide 19: Results : Salammbo
E. Pereira - Simulation of grain morphology evolution during sintering
Extension to chromia doped
Average dihedral angle at 70°
Increase of the neck
Chemical homogenization
  [1]
  [1]
  [2]
Validation on CeO2
19
[1] Ph.D. S. Martin, 2014, « Contribution to the modelling of solid state sintering »
[2] Ph.D. G. I. Nkou Bouala, 2016, «First step of sintering of lanthanides and actinides oxides : an in situ study by ESEM at high temperature»
Notes: AS : Rajouter références

## Slide 20: Results : Salammbo
E. Pereira - Simulation of grain morphology evolution during sintering
Extension to chromia doped
Average dihedral angle at 70°
Increase of the neck
Chemical homogenization
  [1]
  [1]
  [2]
Validation on CeO2
20
[1] Ph.D. S. Martin, 2014, « Contribution to the modelling of solid state sintering »
[2] Ph.D. G. I. Nkou Bouala, 2016, «First step of sintering of lanthanides and actinides oxides : an in situ study by ESEM at high temperature»
Issue with multiple grains phase field approach
Notes: AS : Rajouter références

## Slide 21: Verification : Inferno
E. Pereira - Simulation of grain morphology evolution during sintering
Implement Greenquist model, developed also for UO2 and doped (chromium)
Compare the first results
I. Greenquist and al. «Development of a microstructural grand potential-based sintering model», Computational Materials Science, 2020
21
Notes: Rajouter Références

## Slide 22: Verification : Inferno
Implement Greenquist model, developed also for UO2 and doped (chromium)
Compare the first results
E. Pereira - Simulation of grain morphology evolution during sintering
The concentration in grain must be heterogenous according to [Greenquist et al., 2020]
Must improve the concentration equilibrium computation
22

## Slide 23: Verification : Inferno
Implement Greenquist model, developed also for UO2 and doped (chromium)
Compare the first results
Issue with the equilibrium concentrations
Extend Greenquist method to Uranium diffusion instead of vacancy in order to coupled phase -field with mechanical solver
E. Pereira - Simulation of grain morphology evolution during sintering
23
The concentration in grain must be heterogenous according to [Greenquist et al., 2020]
Must improve the concentration equilibrium computation

## Slide 24: Conclusion & Outlook
3

## Slide 25: Conclusion
Development of multi-species sintering model at RVE scale to study the chromia doped fuel
Work on Salammbo (adaptive meshes):
  Extend model for multi-species sintering
  Further works will be focused on phase-field model due to CPU time and multi-grain issues
First implementation of Greenquist model and verification
E. Pereira - Simulation of grain morphology evolution during sintering
25

## Slide 26: Conclusion
Development of multi-species sintering model at RVE scale to study the chromia doped fuel
Work on Salammbo (adaptive meshes):
  Extend model for multi-species sintering
  Further works will be focused on phase-field model due to CPU time and multi-grain issues
First implementation of Greenquist model and verification
  Extend Greenquist method to Uranium diffusion instead of vacancy
  Benchmark between Salammbo and Inferno
  Coupled phase field method with mechanical solver, compared with multi-grains systems
  Extension to Uranium and doped sintering for phase-field model
E. Pereira - Simulation of grain morphology evolution during sintering
Outlook
26

## Slide 27: Thanks for your attention
Evan Pereira
Evan.PEREIRA@cea.fr

## Slide 28: Context : Sintering of the fuel pellet
Micro-scale behavior :
Mass transport, primarily driven by solid-state diffusion at grains boundaries and surface
⬈ grain size (from 1 to 10 μm up to 5 and 25 μm)
⬊ porosity and number of grains
Macro-scale behavior :
Target O/M stoichiometry close to 2
⬊ volume due to shrinkage (may require adjustment)
⬈ density from ~55% to ~95%
High density
Low density
High density
Residual closed pores are important to trap fission gases within the microstructure.
50 μm
Notes: A relative density of 100% is not the goal, as the residual closed pores serve to trap fission gases within the microstructure.

## Slide 29: Software
SALAMMBO :
Interfaces displacement
INFERNO :
Order parameter
Material based reformulation
MASQUEE
A VOIR SI JE GARDE